An introduction to RADIATION EFFECT ON ELECTRONIC DEVICES
By Francesco Poderico
www.neutronix-ltd.co.uk
francesco@neutronix-ltd.co.uk

---
Kind of Particle in space
Photons
  - Photoelectric
  - Compton scattering
  - Pair production
Particles (Alpha, Proton (p),Beta (β), Photon (X + Gamma ray), Neutron)

---
Photon radiation
Photons are particle representing an electromagnetic wave, composed therefore from a discrete quantum of electromagnetic energy. E= hv
h = Plank constant v = Frequency of electromagnetic wave
Example of photons = X rays, Gamma rays

---
Photoelectric effect
All the energy of the photon (hv) is completely absorbed by the atom, and an orbital electron is ejected
Material	Air	Silicon (Si)	Germanium (Ge)	Silicon Dioxide (SiO₂)
Energy to create a couple electron hole	34 eV	3.6 eV	2.8 eV	17 eV
Ejected
electron
Gamma ray or X ray
E >=(0.5 MeV)

---
Compton scattering effect
Only a partial absorption, from the atom, an orbital electron is ejected + creation of a photon with lower energy
Incident Gamma ray
Scattering photon
E= hv = 0.5 MeV – 3.5 MeV
Photon with lower energy

---
Electron-Positron pair production
Collision with the nucleus
The energy of the incident ray will be split in half (electron + positron) the excess of energy will produce ionization in the travelled material
electron
-
0.51
 MeV e
 MeV e
+
0.51
E >= 1.02 MeV Incident gamma - ray
nucleus
positron

---
ALPHA PARTICLES
Alpha particles are basically Helium nucleus
(the 2 orbit electrons are missing)
Very slow compared with photon, electrons
Produce heavy ionization per centimetre of travel
Travel distance very little ( few centimetres in air, few mm in solid)

---
ALPHA PARTICLES
Creation of alpha particle by decay of an heavy nucleus atom
alpha
Np + alpha
Am

---
Beta particles
Beta decay occurs when the neutron to proton ratio is too great in the nucleus and causes instability.
In simple words beta decay, a neutron is turned into a proton and an electron.

---
Positron radiation
There is also positron emission when the neutron to proton ratio is too small. A proton turns into a neutron and a positron is emitted. A positron is basically a positively charged electron.

---
Maximum Energy of particles in space
Particle type	Maximum Energy
Trapped electrons	10’s of MeV
Trapped protons and Heavy ions	100’s of MeV
Solar Protons	GeV
Solar Heavy Ions	GeV
Galactic cosmic rays	TeV

---
Radiation Damage tree
Cumulative
  - Ionization
    - MOS
    - BJT
  - Displacement
    - BJT
Single Event Effect
  - SEU
    - MOS
  - SEE
    - SEBO
    - SEGR (catastrophic)
    - SEL (catastrophic)

---
Ionization damage
Effect the SiO2 in BJT and MOS
The incident particle creates (directly or indirectly) a hole electron pair, the hole get eventually capture in the SiO2, while the electron can escape. Leaving as result a positive charge in the SiO2 oxide.

---
Ionization (electron-hole creation)
in Si and SiO2
Direct mechanism
  - incident photon (Gamma) create e+/e- pair - incident charged particle (alpha, beta, p) creates an ionization track (along the track of the incident particle itself) releasing energy along the track

---
Ionization (electron-hole creation)
in Si and SiO2
Indirect mechanism
  - an incident heavy particle (alpha, p, Beta) has an elastic collision (no loss of energy) with the nucleus of the Si or SiO2 => creating ionization along the track of the secondary particles

---
Ionization sources

---
LET the e-h generation unit
The quantity of e-h generate depends from
  - The quantity of energy absorbed from the material from unit of length
    1. LET = - dE/dx
    1. LET = - 1/ρ dE/dx (space industry) ρ = material density [kg/m^3]
  - LET represent an instantaneous ionization by a single particle (is used to estimate SEE effects)
  - LET depends on absorbing material, the ionizing particle and on it's energy

---
Effect of radiation on MOS
SiO2 is the most sensible part regarding radiation
Generation of e-h pairs
  - e-h pairs generated in gate and Si substrate will recombine => no effect
  - e-h pairs in SiO2, small part will recombine e- will go through the gate (NMOS) h will go through the SiO2 interface

---
Cumulative Ionization in MOS Oxide, example N-MOS

---
Cumulative Ionization in MOS Oxide, example N-MOS
Vgate
6. holes trapping in the oxide near the Si-SiO2 interface

---
SiO2 INFO
Mobility of electron in SiO2 is 20 cm²/Vs
Mobility of holes is 10^(-4) 10^(-11) cm²/Vs
Energy to create an electron hole pair is between 16 eV and 18 eV

---
Example1: charge estimation on SiO2 due to a single particle
Assuming a particle with a LET = 100 MeV V m²/mg, tox = 1μm, X = 2μm, Y = 3 μm
  1. p = LET/ 18 eV number of electron holes pair by unit of length
  1. ch=p* 1.6 *10^(-19) total charge by unit length
  1. ch * density of SiO2 total charge deposited in SiO2 due to a particle
NOTICE THIS IS NOT ENOUGHT !!! do you know why?

---
Total Ionization Dose (what is a rad?)
The absorbed dose D is equal to the absorbed energy on the unit of mass
  - D = dE/dm [rad]
    - 1 Gy = 100 rad
    - 1 gray = 1 J/kg [m^2/s^2]
Dose rate = absorbed dose for unit of time [rad/s]
A dose must always be referred to the absorbing material, e.g. 100 krad is wrong, 100 krad(SiO2) it's OK

---
Example 2: Total charge on SiO2 due to TID
Assuming a TID = 35 krad, and we know the dimension x,y,z of the SiO2 structure, and the density of SiO2 do you know how to calculate the total charge?

---
Displacement damage (BJT, OPTO)
Caused mainly by Heavy particles (e.g neutrons, protons and electrons)
The incident radiation “moves” the atoms of Si from their original position, changing the characteristics of the material (impurity, extra energetic level)

---
Total Ionization Dose Effects
MOS Transistors
BJT Transistors
JFETs Transistors
Silicon resistors
MOS capacitance

---
TID Effects on MOS
Threshold voltage shift Δvt
Leakage currents
Transductance (gm) decrease

---
TID on N-MOS (on earth)

---
TID on N-MOS effect on Vg after a low TID

---
TID on N-MOS (radiation phase 2)

---
TID on PMOS

---
TID on PMOS

---
Leakage current in N-MOS by TID
Trapped hole charge, cause electron to be attracted by them causing an increase of the Leaked current. Please notice that on P-MOS we don't have this problem!

---
Leakage current between adjacent N-MOS
The leakage current increase even between adjacent N-MOS

---
Reduction of Transconductance due to TID
gm = (2μ Cox Id W/L)½
As the mobility μ change the transconductance change as well
N-MOS and P-MOS in a different way , do you know why?

---
TID effects on NPN BJT

---
TID effects on PNP BJT
In PNP holes e+ trapped in SiO2 migrates near the Si and induce additional interface states.
Β in PNP degrade more than NPN

---
Current gain β vs Ic

---
Displacement effect
BJT Transistors
No effect on MOS (because there is not recombination)
In BJT a displacement creates a recombination current that has the effect of reducing the β

---
Displacement effect

---
Radiation hardness criterion on BJT
(due to displacement damage and TID)
The β decrease because if Ib2, ib3
Ib2 and Ib3 depend from the recombination time of the minority charge τ.
THEREFORE:
If we make sure that the time for a minority charge to pass from the base to the emitter is τ* <<τ we have Ib3* <<Ib3, Ib2*<< Ib2
That's you should use RF BJT

---
Other displacement damage on BJT
VCE saturation decrease
Diodes voltage breakdown decreases.

---
OPTOCOUPLERS
Displacement damage effects:
  - Β gain decreases
  - LED light emission decreases